## Slide 1: Critical Minerals & REE In CCR
Danny L. Gray, P. E. ---- Green Cement, Inc.
March 8, 2022

## Slide 2: CCRs – Abundant CM & REE Resource
Coal Combustion Residuals – Fly Ash, Bottom Ash & Flue Gas Products
Typical Handling Methods – Slurry Impoundments & Landfills
Typical Utilizations – Construction Products – Broad Distribution
Critical Minerals – REE – Typical Conc – 300-800 PPM
Large Volume Production Over Decades of Coal Fired Generation
ACAA Published Annual Production & Use Data – Utilization/Storage
Estimated 1.5 – 3 Billion Tons In Storage Facilities
Small Sites – 1 Million Tons Large Sites 20+Million Tons In Storage

## Slide 3: CCRs – Abundant CM & REE Resource
Coal Combustion Residuals – Fly Ash, Bottom Ash, Slag & Flue Gas Products
Estimated 1.5 – 3 Billion Tons In Storage Facilities
  Typical Storage – Slurry Impoundments & Landfills
  Small Sites – <1 Million Tons; Large Sites 20+Million Tons In Storage
Critical Minerals – REE – Typical Conc – 300-800 PPM
Target Source – Enriched Fly Ash Due To Minerals Processing – Small Particle

## Slide 4: REE & CM In Fly Ash
REE & CM – Higher Concentrations In <200 Fly Ash ( 75 Micron)
Carbon & Sulfur-Flue Gas Products Complicate Processing/Recovery
Central App – Higher REE
Average REE In <200 Mesh – 500 PPM
Simple Assumption -Must Handle 2,000 Ton Per 1 Ton Of Total REE – If All Ore<200 & Perfect Extraction Process

## Slide 5: Large Material Handling Challenge
Broad Distribution – Resources Scattered Over 800+ Facilities
Regulatory Requirements – Impediment For Harvesting
  Solid Waste Permit Sites
  Wastewater Permits
  Air Permits
  RCRA Liabilities Assumption
Dewatering Programs & Drying Required
Centralized Processing w/ Multiple Feedstocks
  Concentration Of Plants In Ohio River Valley
  Water Transport Improves Logistics Cost
Goal To Create Market For Residues From REE/CM Processing
Current CCP Production Trends – Production - Utilization

## Slide 6: Markets - Mature
  Ready Mixed Concrete
  Wallboard
  Roofing Shingles
  Carpet Backing
  Lightweight Plastics
  Lightweight Aggregates
  Agriculture Sulfur Source
  Oil & Gas Drilling

## Slide 7: All CCP Production & Use (1991–2020)

## Slide 8: ACAA Survey Data -

## Slide 9: REE/CM Resources Via CCR Utilization
Large Volume Ore Source
Utilization Brings Environmental Benefits If Coupled With Extraction Processing With Usable Co-Products
Mineral Particle Sizing Completed By Coal Plant Process
Trends In Construction Market Driving Needs To Harvest
Trends In REE/CM Market Driving Demand Growth
Logistics Costs Drive Decisions On Plants